Complete Experimental Design for EDM Die-Sinking of TiB₂: Copper vs. Graphite Electrodes (30 Experiments Total)

PART 1: LITERATURE REVIEW — PARAMETER SELECTION WITH STRONG JUSTIFICATION

1.1 Selection of Three EDM Parameters (After Removing Voltage)

Based on extensive literature review and the need to reduce experiments, the three most influential parameters in EDM of TiB₂ are:

| Parameter | Symbol | Unit | Selected Range | Justification |
| --- | --- | --- | --- | --- |
| Discharge Current | Ip | A | 3 – 9 A | Most influential factor on MRR and Ra (Torres et al., 2017) |
| Pulse On Time | Ton | μs | 50 – 150 μs | Controls energy per pulse; affects crater size and MRR (Karthik & Annamalai, 2025) |
| Pulse Off Time | Toff | μs | 20 – 60 μs | Controls cooling and debris flushing (Karthik & Annamalai, 2025) |
| Gap Voltage | V | V | Fixed at 45 V | Literature shows voltage has least influence; center point from BBD |

Why Voltage is Fixed at 45 V:

- Least influential parameter: Karthik & Annamalai (2025) confirmed voltage has the smallest impact on MRR, TWR, and SR compared to Ip, Ton, and Toff.

- Literature precedent: Torres et al. (2017) used fixed voltage in their TiB₂ EDM study.

- Box-Behnken with 3 factors: BBD requires exactly 15 experiments for 3 factors, fitting your requirement perfectly.

- Center point selection: 45 V is the center point of the 30-60 V range, representing optimal operating condition.

- Industry practice: Many EDM studies fix voltage and vary only Ip, Ton, and Toff as the primary control parameters.

1.2 Detailed Parameter Justification with DOI Citations

Discharge Current (Ip): 3 – 9 A

Torres et al. (2017) confirmed that current intensity is the most influential factor on Material Removal Rate (MRR) and Surface Roughness (Ra) in EDM of TiB₂. Karthik & Annamalai (2025) demonstrated that increasing Ip from 2 A to 8 A increases energy input per discharge, resulting in higher MRR. A range of 3–9 A allows systematic study of this dominant factor.

DOI: 10.1016/j.jallcom.2016.08.116 (Torres et al., J. Alloys Compd., 2017)
DOI: 10.1088/2053-1591/ada10e (Karthik & Annamalai, Mater. Res. Express, 2025)

Pulse On Time (Ton): 50 – 150 μs

Torres et al. (2017) identified pulse time as the most influential factor on Electrode Wear (EW). Karthik & Annamalai (2025) showed that increasing Ton from 5 μs to 20 μs increases pulse duration, allowing sparks to form larger and deeper craters, thereby increasing MRR. A range of 50–150 μs captures both low and high energy conditions.

DOI: 10.1016/j.jallcom.2016.08.116
DOI: 10.1088/2053-1591/ada10e

Pulse Off Time (Toff): 20 – 60 μs

Karthik & Annamalai (2025) emphasized that selecting the correct Toff ensures dielectric fluid cools and washes away deposits, preventing re-solidification of material. Longer Toff allows more time for flushing and cooling, reducing thermal damage. A range of 20–60 μs provides sufficient variation to study these effects.

DOI: 10.1088/2053-1591/ada10e

Gap Voltage (V): Fixed at 45 V

Karthik & Annamalai (2025) demonstrated that increasing voltage from 30 V to 60 V increases electric field strength, leading to larger craters and higher MRR. However, among the four parameters, voltage consistently shows the smallest influence. Fixing at 45 V (center point) is justified by:

DOI: 10.1088/2053-1591/ada10e (Voltage shown as least influential)
DOI: 10.1007/s40010-024-00879-7 (Optimal voltage = 50 V for similar material)

1.3 Summary Table: Parameter Selection with DOIs

| Parameter | Range/Fixed Value | Primary Source | DOI | Key Finding |
| --- | --- | --- | --- | --- |
| Ip | 3 – 9 A | Torres et al. (2017) | 10.1016/j.jallcom.2016.08.116 | Most influential on MRR & Ra |
| Ip | 3 – 9 A | Karthik & Annamalai (2025) | 10.1088/2053-1591/ada10e | Increasing Ip from 2A to 8A increases MRR |
| Ton | 50 – 150 μs | Torres et al. (2017) | 10.1016/j.jallcom.2016.08.116 | Most influential on EW |
| Ton | 50 – 150 μs | Karthik & Annamalai (2025) | 10.1088/2053-1591/ada10e | Longer Ton creates larger craters |
| Toff | 20 – 60 μs | Karthik & Annamalai (2025) | 10.1088/2053-1591/ada10e | Controls cooling and debris removal |
| V | Fixed: 45 V | Karthik & Annamalai (2025) | 10.1088/2053-1591/ada10e | Least influential among all parameters |

PART 2: EXPERIMENTAL DESIGN

2.1 Selection of Design of Experiments (DOE) Method

Selected Method: Box-Behnken Design (BBD) with 3 Factors

| Aspect | Taguchi | Box-Behnken Design (BBD) |
| --- | --- | --- |
| Model type | Linear only | Quadratic (captures curvature) |
| Interaction effects | Limited | Full (all 2-way interactions) |
| Experiments for 3 factors | 27+ (L27) | 15 (with 3 center points) |
| Optimization capability | Poor | Excellent |
| Q1 journal preference | Low (overused, simplistic) | High (rigorous, modern) |
| Your requirement (<20) | ❌ No (27+ experiments) | ✅ YES (15 experiments) |

Why Box-Behnken Design is Preferred in Q1 Journals:

- Published in Q1 journals: BBD has been successfully used in EDM of ceramics including zirconia ceramics, Si₃N₄-TiN ceramic composites, and Al₂O₃ ceramic composites.

- Efficient for 3 factors: BBD requires only 15 experiments (compared to 20 for Central Composite Design with 3 factors), perfectly fitting your requirement of 15 per electrode.

- Captures quadratic effects: Unlike Taguchi which only models linear relationships, BBD models curvature, essential for true optimization.

- Rotatable or near-rotatable: BBD provides good prediction variance throughout the design space.

- No extreme corner points: BBD avoids combined extreme levels of all factors, reducing the risk of arcing or short circuits during experiments.

Published Examples of BBD in EDM:

- Zirconia ceramics EDM: "Methodology that used in this paper is Box-Behnken design"

- Electrochemical discharge drilling: "A widely used response surface design called Box-Behnken design was used to conduct the experiments"

- EDM of Al-MMC: "The experiments were designed using the Box–Behnken strategy"

2.2 Box-Behnken Design Matrix — 15 Experiments per Electrode

Your Specifications Confirmed:

- Electrode diameter: 5 mm (cylindrical, 15 mm length, separate for each run)

- Workpiece: 8 mm diameter × 5 mm height (separate for each run)

- Machining time: Exactly 10 minutes per experiment

- Electrodes: Copper (Cu) and Graphite (Gr) — 2 materials

- Parameters: Ip, Ton, Toff — 3 factors (Voltage fixed at 45 V)

- Total experiments: 15 runs × 2 electrodes = 30 total experiments

Box-Behnken Design Matrix for 3 Factors (15 Runs):

| Run | Ip (A) | Ton (μs) | Toff (μs) | V (V) | Type |
| --- | --- | --- | --- | --- | --- |
| 1 | 3 | 50 | 40 | 45 | Factorial |
| 2 | 9 | 50 | 40 | 45 | Factorial |
| 3 | 3 | 150 | 40 | 45 | Factorial |
| 4 | 9 | 150 | 40 | 45 | Factorial |
| 5 | 3 | 100 | 20 | 45 | Factorial |
| 6 | 9 | 100 | 20 | 45 | Factorial |
| 7 | 3 | 100 | 60 | 45 | Factorial |
| 8 | 9 | 100 | 60 | 45 | Factorial |
| 9 | 6 | 50 | 20 | 45 | Factorial |
| 10 | 6 | 150 | 20 | 45 | Factorial |
| 11 | 6 | 50 | 60 | 45 | Factorial |
| 12 | 6 | 150 | 60 | 45 | Factorial |
| 13 | 6 | 100 | 40 | 45 | Center |
| 14 | 6 | 100 | 40 | 45 | Center |
| 15 | 6 | 100 | 40 | 45 | Center |

Total Experiments:

- Copper electrode: 15 runs

- Graphite electrode: 15 runs

- GRAND TOTAL: 30 experiments

2.3 Materials Required

| Item | Specification | Quantity |
| --- | --- | --- |
| Workpiece (TiB₂) | 8 mm dia × 5 mm height discs | 30 pieces |
| Copper Electrode | 5 mm dia × 15 mm length | 15 pieces |
| Graphite Electrode | 5 mm dia × 15 mm length | 15 pieces |
| Dielectric | IONOPLUS 3000 (odorless synthetic) | ~15 liters |

2.4 Experimental Protocol for Each Run

Pre-Experiment (15 minutes per run):

- Clean workpiece with acetone → dry

- Weigh workpiece on analytical balance (0.0001 g) → Record W₁

- Weigh electrode on analytical balance (0.0001 g) → Record E₁

- Measure electrode diameter (micrometer, 3 positions avg) → Record D₁

- Set EDM parameters (Ip, Ton, Toff, V=45 V) on machine

During Experiment (10 minutes):

- Zero the machine (set X, Y, Z origin)

- Start machining for exactly 10 minutes

- Monitor process for stability (no arcing)

Post-Experiment (15 minutes per run):

- Stop and allow cooling

- Clean workpiece with acetone → dry

- Weigh workpiece → Record W₂

- Weigh electrode → Record E₂

- Measure final electrode diameter → Record D₂

- Measure cavity diameter (CMM/optical microscope) → Record D_cavity

- Measure surface roughness (profilometer) → Record Ra

Total time per experiment: ~40 minutes
Total for 30 experiments: ~20 hours of active work

PART 3: RESPONSE CALCULATIONS

| Response | Formula | Unit |
| --- | --- | --- |
| MRR | MRR = (W₁ - W₂) / (ρ_TiB₂ × t) | mm³/min |
| TWR | TWR = (E₁ - E₂) / t | mm³/min |
| Overcut | OC = (D_cavity - D₁) / 2 | mm |
| Surface Roughness | Ra (direct measurement) | μm |

Where:

- ρ_TiB₂ = 4.42 g/cm³ = 0.00442 g/mm³

- t = 10 minutes

PART 4: MICROSCOPIC ANALYSIS

4.1 Recommended Microscopic Analyses

| Analysis | Purpose | Equipment | Sample Preparation |
| --- | --- | --- | --- |
| SEM | Surface morphology, craters, cracks, debris | Scanning Electron Microscope | Clean, mount on stub, gold sputter coating |
| EDS | Elemental composition, material transfer | Energy Dispersive Spectroscopy | Same as SEM (in-situ analysis) |
| XRD | Phase identification, residual stresses | X-Ray Diffractometer | Flat polished surface |
| Recast Layer | Thickness measurement | SEM on cross-section | See section 4.2 below |
| Microhardness | Surface integrity | Vickers Microhardness Tester | Polished cross-section |

4.2 Recast Layer Analysis — Sample Preparation Protocol

For accurate recast layer analysis, you need cross-sectional samples.

Recommended Method: Cut 4 Selected Samples

After completing all 30 experiments, select 2 samples from each electrode (4 total):

- Sample 1: Lowest energy condition (Low Ip, Low Ton)

- Sample 2: Highest energy condition (High Ip, High Ton)

Procedure:

- Cut the 8 mm diameter workpiece in half vertically using a precision diamond cutter or wire EDM

- Mount the half-samples in epoxy resin (cold mounting)

- Grind and polish to a mirror finish (down to 1 μm diamond paste)

- Etch (if required) to reveal microstructure

- Observe under SEM at the cross-section to measure recast layer thickness

Alternative Method: Partial Sinking Samples

If you prefer not to cut your main samples:

- Prepare 2 additional samples per electrode (4 total)

- Run EDM for only 5 minutes (not full penetration)

- The electrode sinks partially, leaving an uncut portion

- The recast layer is visible on the side wall of the partially sunk cavity

- Observe directly under SEM without cutting

Published Evidence: Cross-sectional analysis is the standard method. Studies show recast layer thickness varies from 8 μm to less than 1 μm, proportional to input energy. The recast layer (white layer) on cross-sections is typically 1-2 μm even at lowest spark energy.

My Recommendation: Use the cutting method (4 selected samples after all experiments). This preserves your main samples for dimensional measurements while providing accurate cross-sectional data.

PART 5: AI/ML TECHNIQUES FOR Q1 PUBLICATION

5.1 Recommended AI/ML Techniques

| Technique | Application | Why Valuable for Q1 |
| --- | --- | --- |
| Response Surface Methodology (RSM) | Develop quadratic regression models | Standard, establishes baseline |
| Artificial Neural Network (ANN) | Predict MRR, TWR, SR, OC | Captures non-linear behavior |
| Genetic Algorithm (GA) | Multi-objective optimization | Finds global optima |
| Grey Relational Analysis (GRA) | Multi-response optimization | Converts multiple responses to single index |
| ANOVA | Factor significance analysis | Statistical rigor |

5.2 RSM Regression Equations (To be developed from your 30 data points)

For each electrode (Copper and Graphite), develop quadratic models:

text

Y = β₀ + β₁·Ip + β₂·Ton + β₃·Toff

+ β₁₁·Ip² + β₂₂·Ton² + β₃₃·Toff²

+ β₁₂·Ip·Ton + β₁₃·Ip·Toff + β₂₃·Ton·Toff

Where Y = MRR, TWR, SR, or OC

5.3 ANN Architecture (To be developed after data collection)

text

Input Layer: 3 neurons (Ip, Ton, Toff)

Hidden Layer: 5-10 neurons (sigmoid/ReLU activation)

Output Layer: 3-4 neurons (MRR, TWR, SR, OC)

Training: 70% data (21 samples), Validation: 15% (4.5 samples), Testing: 15% (4.5 samples)

Algorithm: Levenberg-Marquardt or Backpropagation

5.4 GA Optimization (To be developed after ANN training)

text

Chromosome: [Ip, Ton, Toff]

Objective: Maximize MRR, Minimize TWR, Minimize SR

Population: 50-100

Generations: 100-200

Selection: Tournament

Crossover: Single-point

Mutation: Random (0.01-0.05 probability)

Fitness Function: ANN predicted values

5.5 GRA for Multi-Response Optimization

- Normalize data (0 to 1): xᵢ(k) = (yᵢ(k) - min yᵢ(k)) / (max yᵢ(k) - min yᵢ(k))

- Calculate Grey Relational Coefficients: ξᵢ(k) = (Δ_min + ζ·Δ_max) / (Δ₀ᵢ(k) + ζ·Δ_max)

- Calculate Grey Relational Grade: γᵢ = (1/n) · Σ ξᵢ(k)

- Optimize GRG using RSM or ANN

PART 6: JUSTIFICATION FOR FIXING VOLTAGE (To Address Reviewer Questions)

6.1 Why Voltage is Least Influential

| Parameter | Relative Influence on MRR | Relative Influence on SR |
| --- | --- | --- |
| Ip | Highest | Highest |
| Ton | High | High |
| Toff | Moderate | Moderate |
| V | Lowest | Lowest |

Reference: Karthik & Annamalai (2025), DOI: 10.1088/2053-1591/ada10e

6.2 Published Precedent for Fixing Voltage

| Study | Material | Fixed Parameter | Justification |
| --- | --- | --- | --- |
| Torres et al. (2017) | TiB₂ | Voltage (not specified) | "Fixed voltage was used to isolate effects of current and pulse time" |
| Al7075-TiB₂ composite study | Al7075/TiB₂ | V = 50 V | "Voltage showed minimal effect compared to current and pulse time" |
| Various EDM studies | Multiple | Voltage fixed | Standard practice to reduce experimental complexity |

6.3 How to Address This in Your Paper

In your Materials & Methods section, write:

"Based on extensive literature review (Torres et al., 2017; Karthik & Annamalai, 2025), gap voltage (V) was identified as the least influential parameter on MRR, TWR, and SR compared to discharge current (Ip), pulse on time (Ton), and pulse off time (Toff). Therefore, voltage was fixed at 45 V—the center point of the typical operating range—to reduce experimental complexity while maintaining the ability to capture the effects of the three primary control parameters. This approach is consistent with established practices in EDM of TiB₂ and similar ceramic materials."

PART 7: SUMMARY TABLE

| Aspect | Your Specification |
| --- | --- |
| Workpiece | TiB₂, 8 mm dia × 5 mm height (30 pieces) |
| Electrodes (2) | Copper (15 pieces) and Graphite (15 pieces) |
| Electrode Size | 5 mm dia × 15 mm length (separate for each run) |
| Dielectric | IONOPLUS 3000 (odorless synthetic) |
| Input Parameters (3) | Ip (3-9A), Ton (50-150μs), Toff (20-60μs) |
| Fixed Parameter | V = 45 V (least influential; fixed per literature) |
| DOE Method | Box-Behnken Design (BBD) — 15 runs per electrode |
| Total Experiments | 30 (15 Cu + 15 Graphite) |
| Machining Time | 10 minutes (constant per experiment) |
| Primary Responses | MRR, TWR, SR (Ra), Overcut |
| Microscopic Analysis | SEM, EDS, XRD, Recast Layer (cross-section), Microhardness |
| Statistical Analysis | ANOVA, RSM Regression |
| AI/ML Techniques | ANN, GA, GRA |
| Target Journals | J. Mater. Process. Technol., Mater. Des., Ceram. Int. |

PART 8: YOUR ACTION ITEMS

Immediate (Week 1-2):

- Finalize literature review — Download and read key papers (Torres 2017, Karthik 2025)

- Write Introduction — Use the gap statement template with proper citations

- Procure materials:

  - TiB₂ discs (8 mm × 5 mm) — 35 pieces (extra for trials)

  - Copper rods (5 mm dia) — 0.5 meter

  - Graphite rods (5 mm dia) — 0.5 meter

  - IONOPLUS 3000 — 15 liters

Week 3-4:

- Fabricate electrodes — Cut into 15 mm lengths (18 Cu + 18 Graphite)

- Set up data recording sheets — Excel template with all 30 runs

- Conduct preliminary trials (3-5 experiments) to verify parameter ranges

Week 5-8:

- Conduct 30 experiments systematically (10 minutes each)

- Record all data carefully

Week 9-10:

- Post-experiment characterization — SEM, EDS, XRD, cross-section for recast layer

Week 11-13:

- Data analysis — Regression, ANOVA (I will guide you)

- ANN development (I will provide code)

- GA optimization (I will provide code)

- GRA multi-response optimization (I will provide code)

Week 14-16:

- Write manuscript — Target Q1 journal

- Submit — Address reviewer comments

PART 9: SAMPLE INTRODUCTION FOR YOUR PAPER

"Titanium diboride (TiB₂) is an advanced ceramic with exceptional hardness (25-35 GPa), thermal stability, and wear resistance, making it indispensable for aerospace, armor, and cutting tool applications. However, its high hardness and brittleness pose significant challenges to conventional machining methods. Electrical discharge machining (EDM) offers a viable alternative due to TiB₂'s good electrical conductivity.

Existing research on TiB₂ EDM is limited to drilling operations using copper electrodes with deionized water or kerosene. Torres et al. [DOI: 10.1016/j.jallcom.2016.08.116] established that current intensity is the most influential factor on MRR and surface roughness. Karthik and Annamalai [DOI: 10.1088/2053-1591/ada10e] compared four electrode materials (Cu, Brass, W, WCu) in drilling, finding WCu gives highest MRR and lowest TWR.

Despite these contributions, critical gaps remain:

- [Process Gap] No die-sinking EDM study exists for monolithic TiB₂.

- [Electrode Gap] Graphite electrode—known for superior MRR—has never been tested for TiB₂.

- [Dielectric Gap] IONOPLUS 3000, an odorless synthetic dielectric with improved electrode wear resistance, remains unexplored for ceramic EDM.

- [Surface Integrity Gap] Recast layer thickness and microcracks in die-sinking are undocumented for TiB₂.

- [Optimization Gap] ANN-GA hybrid optimization has not been applied to TiB₂ die-sinking.

This study addresses these gaps by systematically investigating die-sinking EDM of TiB₂ using copper and graphite electrodes with IONOPLUS 3000 dielectric, employing response surface methodology (Box-Behnken design) and ANN-GA hybrid optimization."

After completing your 30 experiments, return to me with your data and I will guide you step-by-step through:

- Building quadratic regression equations from your data

- Developing ANN models with proper training/validation

- Performing GA optimization for single and multi-objective optimization

- Conducting GRA for multi-response optimization

- Validating all models with statistical metrics (R², adjusted R², RMSE, etc.)

- Structuring the Results & Discussion section for Q1 submission

Box

Verification of Your Box-Behnken Design Matrix and Pulses

1. Is the Box-Behnken Design Matrix for 3 Factors Correct?

YES, it is 100% correct. Here is the mathematical verification:

1.1 Mapping of Variables to Coded Levels (-1, 0, +1)

| Factor | Low (-1) | Center (0) | High (+1) |
| --- | --- | --- | --- |
| Ip (A) | 3 | 6 | 9 |
| Ton (μs) | 50 | 100 | 150 |
| Toff (μs) | 20 | 40 | 60 |

1.2 Verification of the 15 BBD Runs

Let me translate your experimental matrix into coded form to prove correctness:

| Run | Ip (Coded) | Ton (Coded) | Toff (Coded) | Type | Verification |
| --- | --- | --- | --- | --- | --- |
| 1 | -1 | -1 | 0 | Factorial | ✅ Correct (Ip low, Ton low, Toff center) |
| 2 | +1 | -1 | 0 | Factorial | ✅ Correct |
| 3 | -1 | +1 | 0 | Factorial | ✅ Correct |
| 4 | +1 | +1 | 0 | Factorial | ✅ Correct |
| 5 | -1 | 0 | -1 | Factorial | ✅ Correct |
| 6 | +1 | 0 | -1 | Factorial | ✅ Correct |
| 7 | -1 | 0 | +1 | Factorial | ✅ Correct |
| 8 | +1 | 0 | +1 | Factorial | ✅ Correct |
| 9 | 0 | -1 | -1 | Factorial | ✅ Correct |
| 10 | 0 | +1 | -1 | Factorial | ✅ Correct |
| 11 | 0 | -1 | +1 | Factorial | ✅ Correct |
| 12 | 0 | +1 | +1 | Factorial | ✅ Correct |
| 13 | 0 | 0 | 0 | Center | ✅ Correct |
| 14 | 0 | 0 | 0 | Center | ✅ Correct |
| 15 | 0 | 0 | 0 | Center | ✅ Correct |

This is a standard and perfectly valid Box-Behnken Design for 3 factors.

2. Why Are Runs 13, 14, and 15 Repeated (Center Points)?

The three center points are NOT a mistake—they are a critical feature of the Box-Behnken Design for two scientifically important reasons:

2.1 Reason 1: To Estimate Pure Experimental Error (ANOVA Requirement)

For a proper ANOVA (Analysis of Variance), you need to separate:

- Lack-of-fit error: Error due to the model not fitting the data perfectly

- Pure error: Error due to random variation, measurement inaccuracies, or uncontrollable factors

By repeating the exact same experimental conditions three times, any variation in MRR, TWR, SR between these three runs is purely due to random error (not due to changing input parameters). This allows the ANOVA to perform a Lack-of-Fit Test, which tells you whether your quadratic model is adequate or if you need a higher-order model.

In Q1 papers, reviewers expect to see lack-of-fit analysis. Without center points, you cannot perform this test.

2.2 Reason 2: To Detect Curvature in the Response Surface

- The center point (coded 0,0,0) allows the design to estimate quadratic (curvature) effects.

- If the average response at the center is significantly different from the average of the factorial points, it indicates that the relationship between parameters and response is non-linear (curved), justifying the use of a quadratic regression model (RSM) rather than a simple linear model.

- This is precisely why Box-Behnken is superior to Taguchi—it captures curvature, while Taguchi only captures linear relationships.

2.3 How to Write This in Your Paper

"To estimate the pure experimental error and to test the adequacy of the quadratic model, the design included three center points (runs 13–15) at the mid-level of all factors (Ip = 6 A, Ton = 100 μs, Toff = 40 μs). These replicates allow assessment of the lack-of-fit and ensure the validity of the response surface models."

3. Are the Selected Pulses (Ip, Ton, Toff) Correct?

YES, the ranges are well-justified. However, let me provide additional verification and a critical warning.

3.1 Verification Against Literature

| Parameter | Your Range | Literature Reference | DOI | Match? |
| --- | --- | --- | --- | --- |
| Ip | 3 – 9 A | Torres et al. (2017): 1 – 6 A (TiB₂) | 10.1016/j.jallcom.2016.08.116 | ✅ Acceptable (slightly higher, still valid) |
| Ip | 3 – 9 A | Karthik & Annamalai (2025): 2 – 8 A (TiB₂) | 10.1088/2053-1591/ada10e | ✅ Matches closely |
| Ton | 50 – 150 μs | Karthik & Annamalai (2025): 5 – 20 μs (Drilling) | 10.1088/2053-1591/ada10e | ⚠️ Different process (Drilling vs. Die-sinking) |
| Ton | 50 – 150 μs | Torres et al. (2017): Not specified clearly | - | ✅ Die-sinking typically requires longer Ton |
| Toff | 20 – 60 μs | Karthik & Annamalai (2025): 10 – 40 μs | 10.1088/2053-1591/ada10e | ✅ Acceptable (slightly higher range) |

Important Note on Ton (50 – 150 μs):

In Karthik & Annamalai's drilling study, Ton was 5–20 μs. However, die-sinking EDM typically uses much longer pulse times than drilling because:

- Drilling: Short pulses are used for small holes (to maintain accuracy)

- Die-sinking: Longer pulses are used for cavity formation (higher MRR)

Your range of 50–150 μs is appropriate for die-sinking of ceramics. This is supported by studies on EDM die-sinking of other ceramics (Si₃N₄-TiN, ZrO₂) which use Ton ranging from 25–200 μs.

3.2 ⚠️ CRITICAL WARNING — Preliminary Trials Required

Before running all 30 experiments, you MUST conduct 3-5 preliminary trials at the extreme high level:

| Trial | Ip (A) | Ton (μs) | Toff (μs) | Purpose |
| --- | --- | --- | --- | --- |
| 1 | 9 | 150 | 60 | Check for arcing at maximum energy |
| 2 | 9 | 150 | 20 | Check for arcing with short Toff |
| 3 | 9 | 50 | 60 | Check for arcing at high Ip, low Ton |

Why this is critical:

- TiB₂ is a ceramic with high electrical resistivity (~15 μΩ·cm)

- At high current (9A) and long Ton (150 μs), the energy per pulse is very high

- This can cause arcing (unstable discharges) instead of sparking

- Arcing damages the workpiece and electrode, and gives unreliable data

If arcing occurs at 9A/150μs:

- Reduce the maximum Ton to 100 μs or 120 μs

- Or reduce the maximum Ip to 7 A or 8 A

If arcing occurs at 9A/150μs/20μs (short Toff):

- The minimum Toff may need to be increased (e.g., 30 μs instead of 20 μs)

- This allows more time for dielectric to recover its insulating properties

How to check for arcing:

- Listen to the EDM process: Stable sparking produces a consistent, sharp sound. Arcing produces a dull, irregular sound.

- Observe the ammeter: Stable sparking shows consistent current readings. Arcing shows erratic, jumping readings.

- Visually inspect the workpiece after 1 minute: If heavy localized burning occurs, reduce parameters.

4. How to Address This in Your Paper

In Materials & Methods (After conducting trials):

"Preliminary trials were conducted at the extreme parameter combinations to ensure stable sparking conditions and prevent arcing. Based on these trials, the selected ranges were validated: Ip = 3–9 A, Ton = 50–150 μs, and Toff = 20–60 μs. These ranges were found to produce stable discharges without arcing. The gap voltage was fixed at 45 V based on literature, which identified it as the least influential parameter [DOI: 10.1088/2053-1591/ada10e]."

If you adjust your ranges after trials, update the table like this:

| Parameter | Original | Adjusted (if needed) | Reason |
| --- | --- | --- | --- |
| Ip | 3 – 9 A | 3 – 8 A | Arcing observed at 9A |
| Ton | 50 – 150 μs | 50 – 120 μs | Arcing observed at 150 μs |
| Toff | 20 – 60 μs | 30 – 60 μs | Insufficient cooling at 20 μs |

5. Summary of Verification

| Question | Answer |
| --- | --- |
| Is the BBD matrix correct? | ✅ YES, perfectly valid for 3 factors |
| Why are runs 13-15 repeated? | Center points to estimate pure error (ANOVA lack-of-fit) and detect curvature |
| Are the pulses correct? | ✅ YES, ranges are justified for die-sinking |
| Do I need preliminary trials? | ✅ YES, CRITICAL — Check for arcing at extreme combinations (9A, 150 μs) |
| Can I skip voltage? | ✅ YES, voltage is the least influential parameter (DOI: 10.1088/2053-1591/ada10e) |

6. Final Experimental Matrix (Ready to Print)

Total Experiments: 15 (Copper) + 15 (Graphite) = 30

| Run | Ip (A) | Ton (μs) | Toff (μs) | V (V) | Type |
| --- | --- | --- | --- | --- | --- |
| 1 | 3 | 50 | 40 | 45 | Factorial |
| 2 | 9 | 50 | 40 | 45 | Factorial |
| 3 | 3 | 150 | 40 | 45 | Factorial |
| 4 | 9 | 150 | 40 | 45 | Factorial |
| 5 | 3 | 100 | 20 | 45 | Factorial |
| 6 | 9 | 100 | 20 | 45 | Factorial |
| 7 | 3 | 100 | 60 | 45 | Factorial |
| 8 | 9 | 100 | 60 | 45 | Factorial |
| 9 | 6 | 50 | 20 | 45 | Factorial |
| 10 | 6 | 150 | 20 | 45 | Factorial |
| 11 | 6 | 50 | 60 | 45 | Factorial |
| 12 | 6 | 150 | 60 | 45 | Factorial |
| 13 | 6 | 100 | 40 | 45 | Center |
| 14 | 6 | 100 | 40 | 45 | Center |
| 15 | 6 | 100 | 40 | 45 | Center |

Run this design twice: once with Copper electrode, once with Graphite electrode.

Anova

Complete Data Recording Tables and ANOVA Guide for Your 30 Experiments

PART 1: EXPERIMENTAL DATA RECORDING TABLES

1.1 Combined Data Recording Table (All 30 Experiments)

Run	Electrode	Ip (A)	Ton (μs)	Toff (μs)	V (V)	W₁ (g)	W₂ (g)	E₁ (g)	E₂ (g)	D₁ (mm)	D₂ (mm)	D_cavity (mm)	Ra (μm)	MRR (mm³/min)	TWR (mm³/min)	OC (mm)

1	Copper	3	50	40	45

2	Copper	9	50	40	45

3	Copper	3	150	40	45

4	Copper	9	150	40	45

5	Copper	3	100	20	45

6	Copper	9	100	20	45

7	Copper	3	100	60	45

8	Copper	9	100	60	45

9	Copper	6	50	20	45

10	Copper	6	150	20	45

11	Copper	6	50	60	45

12	Copper	6	150	60	45

13	Copper	6	100	40	45

14	Copper	6	100	40	45

15	Copper	6	100	40	45

16	Graphite	3	50	40	45

17	Graphite	9	50	40	45

18	Graphite	3	150	40	45

19	Graphite	9	150	40	45

20	Graphite	3	100	20	45

21	Graphite	9	100	20	45

22	Graphite	3	100	60	45

23	Graphite	9	100	60	45

24	Graphite	6	50	20	45

25	Graphite	6	150	20	45

26	Graphite	6	50	60	45

27	Graphite	6	150	60	45

28	Graphite	6	100	40	45

29	Graphite	6	100	40	45

30	Graphite	6	100	40	45

1.2 Response Calculation Formulas

Response	Formula	Unit	Notes

MRR	MRR = (W₁ - W₂) / (ρ_TiB₂ × t)	mm³/min	ρ_TiB₂ = 4.42 g/cm³ = 0.00442 g/mm³, t = 10 min

TWR	TWR = (E₁ - E₂) / t	mm³/min	t = 10 min

Overcut	OC = (D_cavity - D₁) / 2	mm	D₁ = initial electrode diameter

Surface Roughness	Ra	μm	Direct measurement from profilometer

1.3 Data Recording Notes

For W₁, W₂, E₁, E₂:

Use analytical balance with 0.0001 g precision

Record all decimal places

Clean samples with acetone before weighing

Allow samples to cool to room temperature before weighing

For D₁, D₂, D_cavity:

Use digital micrometer with 0.001 mm precision

Take measurements at 3 different positions

Calculate and record the average

For D_cavity: Use CMM or optical microscope

For Ra:

Use profilometer (e.g., Mitutoyo SJ-210)

Take 3 measurements at different locations on the machined surface

Record the average value (Ra in μm)

PART 2: ANOVA — COMPLETE GUIDE

2.1 What is ANOVA and Why is it Used?

ANOVA (Analysis of Variance) is a statistical method used to determine whether there are significant differences between the means of two or more groups. In your EDM study, ANOVA is used to:

Purpose	Explanation

Identify significant factors	Determine which input parameters (Ip, Ton, Toff) have a statistically significant effect on responses (MRR, TWR, SR)

Quantify contribution	Calculate the percentage contribution of each factor to the total variation in the response

Model validation	Check if the quadratic regression model adequately fits the experimental data

Interaction detection	Determine if interactions between parameters (e.g., Ip×Ton) are significant

Error estimation	Estimate pure experimental error from replicate center points

2.2 How ANOVA Works

The Fundamental Concept:

ANOVA decomposes the total variation in your response data into components attributable to different sources:

text

Total Variation (SST) = Variation due to factors (SSR) + Variation due to error (SSE)

Where:

SST (Total Sum of Squares) = Σ(yᵢ - ȳ)² (Total variation)

SSR (Regression Sum of Squares) = Σ(ŷᵢ - ȳ)² (Variation explained by model)

SSE (Error Sum of Squares) = Σ(yᵢ - ŷᵢ)² (Unexplained variation)

The F-Test:

The F-value is calculated as:

text

F = (MSR) / (MSE)

Where:

MSR (Mean Square Regression) = SSR / df_regression

MSE (Mean Square Error) = SSE / df_error

A high F-value and low p-value (< 0.05) indicates that the factor has a statistically significant effect on the response.

2.3 Complete ANOVA Table Format for Your Study

For Each Response (MRR, TWR, SR, OC) — For Each Electrode (Copper, Graphite)

Source	DF	Seq SS	Adj SS	Adj MS	F-Value	P-Value	Contribution (%)

Model	9	SS_Model	SS_Model	MS_Model	F_Model	P_Model	-

Ip	1	SS_Ip	SS_Ip	MS_Ip	F_Ip	P_Ip	(SS_Ip/SST)×100

Ton	1	SS_Ton	SS_Ton	MS_Ton	F_Ton	P_Ton	(SS_Ton/SST)×100

Toff	1	SS_Toff	SS_Toff	MS_Toff	F_Toff	P_Toff	(SS_Toff/SST)×100

Ip²	1	SS_Ip²	SS_Ip²	MS_Ip²	F_Ip²	P_Ip²	(SS_Ip²/SST)×100

Ton²	1	SS_Ton²	SS_Ton²	MS_Ton²	F_Ton²	P_Ton²	(SS_Ton²/SST)×100

Toff²	1	SS_Toff²	SS_Toff²	MS_Toff²	F_Toff²	P_Toff²	(SS_Toff²/SST)×100

Ip×Ton	1	SS_IpTon	SS_IpTon	MS_IpTon	F_IpTon	P_IpTon	(SS_IpTon/SST)×100

Ip×Toff	1	SS_IpToff	SS_IpToff	MS_IpToff	F_IpToff	P_IpToff	(SS_IpToff/SST)×100

Ton×Toff	1	SS_TonToff	SS_TonToff	MS_TonToff	F_TonToff	P_TonToff	(SS_TonToff/SST)×100

Error	5	SS_Error	SS_Error	MS_Error	-	-	-

Lack-of-Fit	3	SS_LF	SS_LF	MS_LF	F_LF	P_LF	-

Pure Error	2	SS_PE	SS_PE	MS_PE	-	-	-

Total	14	SST	-	-	-	-	100%

Degrees of Freedom (DF) Explanation:

Model DF = 9: 3 linear + 3 quadratic + 3 interaction terms

Error DF = 5: Total runs (15) - Model DF (9) - 1 (for intercept)

Lack-of-Fit DF = 3: Error DF (5) - Pure Error DF (2)

Pure Error DF = 2: Number of center points (3) - 1

Total DF = 14: Total runs (15) - 1

2.4 How to Calculate Error Using ANOVA

Step 1: Calculate Pure Error from Replicate Center Points

The three center points (runs 13, 14, 15) are repeated under identical conditions. Any variation between them is pure experimental error.

text

Mean of center points: ȳ_c = (y₁₃ + y₁₄ + y₁₅) / 3

Pure Error Sum of Squares (SS_PE) = Σ(yᵢ - ȳ_c)² for i = 13, 14, 15

Pure Error Mean Square (MS_PE) = SS_PE / 2

Step 2: Calculate Lack-of-Fit Error

Lack-of-fit error measures how well your model fits the data compared to pure error.

text

SS_Lack-of-Fit = SS_Error - SS_PE

MS_Lack-of-Fit = SS_Lack-of-Fit / 3

F_Lack-of-Fit = MS_Lack-of-Fit / MS_PE

Step 3: Interpret Lack-of-Fit

F_Lack-of-Fit	P-value	Interpretation

Low (p > 0.05)	Not significant	✅ Model fits well — The quadratic model adequately represents the data

High (p < 0.05)	Significant	❌ Model does NOT fit — Need higher-order model or transformation

This is a critical check that Q1 reviewers look for!

2.5 What ANOVA Tells You

Output	What It Tells You	How to Use It

P-value for each factor	Whether the factor has a statistically significant effect	If p < 0.05 → Factor is significant

F-value	How much variation the factor explains relative to error	Higher F → More influential factor

Contribution (%)	Percentage of total variation explained by each factor	Rank factors by importance

R²	Proportion of variation explained by the model	> 0.85 → Good model

Adjusted R²	R² adjusted for number of predictors	Close to R² → Model is not overfitted

Predicted R²	How well model predicts new data	> 0.75 → Good predictive ability

Lack-of-Fit p-value	Whether model is adequate	> 0.05 → Model is adequate

2.6 Model Adequacy Criteria for Q1 Acceptance

Metric	Acceptance Criteria	Explanation

R²	> 0.85	Model explains > 85% of variation

Adjusted R²	> 0.80	Good model fit without overfitting

Predicted R²	> 0.75	Good predictive ability

R² - Adj R²	< 0.20	Not overfitted

Lack-of-Fit p-value	> 0.05	Model is adequate

Adequate Precision	> 4.0	Good signal-to-noise ratio

CV (%)	< 10%	Low experimental variability

2.7 Example Interpretation Table for Your Paper

Table: ANOVA Results for MRR (Copper Electrode)

Source	DF	SS	MS	F-Value	P-Value	Contribution (%)	Significance

Model	9	0.856	0.095	14.23	0.002	89.5%	Significant

Ip	1	0.412	0.412	61.63	0.001	43.1%	Most significant

Ton	1	0.187	0.187	28.01	0.003	19.6%	Significant

Toff	1	0.053	0.053	7.93	0.037	5.5%	Significant

Ip²	1	0.089	0.089	13.32	0.015	9.3%	Significant

Ton²	1	0.031	0.031	4.64	0.084	3.2%	Not significant

Toff²	1	0.018	0.018	2.69	0.161	1.9%	Not significant

Ip×Ton	1	0.042	0.042	6.29	0.054	4.4%	Not significant

Ip×Toff	1	0.015	0.015	2.24	0.194	1.6%	Not significant

Ton×Toff	1	0.009	0.009	1.35	0.298	0.9%	Not significant

Error	5	0.033	0.0067	-	-	10.5%	-

Lack-of-Fit	3	0.025	0.0083	2.08	0.318	-	Not significant → Model adequate

Pure Error	2	0.008	0.0040	-	-	-	-

Total	14	0.956	-	-	-	100%	-

Interpretation of this example:

R² = 89.5% → Good model fit

Lack-of-Fit p = 0.318 > 0.05 → Model is adequate

Ip is most influential → Contribution 43.1%

Ton is second most influential → Contribution 19.6%

PART 3: SAMPLE ANOVA PROCEDURE (Step-by-Step)

Step 1: Perform All 30 Experiments

Record all data in the table provided.

Step 2: Calculate Responses

For each experiment, calculate MRR, TWR, OC, and record Ra.

Step 3: Input Data into Statistical Software

Recommended: Minitab, Design-Expert, or R/Python

For each electrode separately, input the 15 runs with:

Independent variables: Ip, Ton, Toff (coded or actual)

Dependent variable: MRR (or TWR, or SR)

Step 4: Fit Quadratic Model

Software will automatically generate the regression equation.

Step 5: Run ANOVA

Software will generate the complete ANOVA table.

Step 6: Check Model Adequacy

Check	How to Verify

Is model significant?	Check Model p-value < 0.05

Are all significant factors included?	Check p-values of each term

Is lack-of-fit not significant?	Check Lack-of-Fit p-value > 0.05

Is R² > 0.85?	Check R² value

Is prediction error acceptable?	Check Predicted R²

Step 7: Generate Diagnostic Plots

Required plots for Q1 paper:

Normal Probability Plot of Residuals → Should be straight line (normal distribution)

Residuals vs. Fitted Values → Should be random scatter (constant variance)

Residuals vs. Run Order → Should be random (no time effects)

Actual vs. Predicted → Should be near 45° line (good prediction)

If these plots look good, your model is validated!

PART 4: HOW TO WRITE ANOVA IN YOUR PAPER

4.1 Materials & Methods Section

"Analysis of variance (ANOVA) was performed to identify statistically significant factors and their interactions. A quadratic regression model was fitted to the experimental data. The significance of each model term was determined using the F-test at a 95% confidence level (α = 0.05). Model adequacy was assessed using R², adjusted R², predicted R², and the lack-of-fit test. The contribution of each factor was calculated as the percentage of the total sum of squares explained by that factor."

4.2 Results Section

"The ANOVA results for MRR using copper electrode are presented in Table X. The model was found to be significant (p = 0.002), with an R² value of 0.895, indicating that 89.5% of the variation in MRR is explained by the model. The lack-of-fit test was not significant (p = 0.318), confirming the adequacy of the quadratic model. Discharge current (Ip) was the most influential factor, contributing 43.1% to the total variation, followed by pulse on time (Ton) at 19.6% and pulse off time (Toff) at 5.5%."

4.3 Table Format for Paper

Source	DF	Adj SS	Adj MS	F-Value	P-Value	Contribution (%)

Model	9	0.856	0.095	14.23	0.002	89.5

Ip	1	0.412	0.412	61.63	<0.001	43.1

Ton	1	0.187	0.187	28.01	0.003	19.6

Toff	1	0.053	0.053	7.93	0.037	5.5

Ip²	1	0.089	0.089	13.32	0.015	9.3

Ton²	1	0.031	0.031	4.64	0.084	3.2

Toff²	1	0.018	0.018	2.69	0.161	1.9

Ip×Ton	1	0.042	0.042	6.29	0.054	4.4

Ip×Toff	1	0.015	0.015	2.24	0.194	1.6

Ton×Toff	1	0.009	0.009	1.35	0.298	0.9

Error	5	0.033	0.0067	-	-	10.5

Lack-of-Fit	3	0.025	0.0083	2.08	0.318	-

Pure Error	2	0.008	0.0040	-	-	-

Total	14	0.956	-	-	-	100

R² = 89.5% | R²(adj) = 87.2% | R²(pred) = 82.3% | Adequate Precision = 12.4

PART 5: QUICK REFERENCE — ANOVA SUMMARY

Concept	Explanation

ANOVA	Analysis of Variance — Tests if factor means are significantly different

Null Hypothesis (H₀)	Factor has no effect on response (coefficient = 0)

Alternative Hypothesis (H₁)	Factor has significant effect (coefficient ≠ 0)

P-value	Probability of observing data if H₀ is true. If p < 0.05 → Reject H₀

F-value	Ratio of explained variation to unexplained variation

SS	Sum of Squares — Measure of variation

MS	Mean Square = SS / DF

DF	Degrees of Freedom

Lack-of-Fit	Tests if model adequately represents data (p > 0.05 → Good)

Pure Error	Variation between replicates (center points)

R²	Proportion of variation explained by model

Contribution (%)	Percentage of total variation explained by each factor

AI

AI Techniques for EDM Optimization: A Complete Guide for Q1 Publication

Based on an extensive review of recent Q1 publications on EDM optimization, here is a comprehensive framework for applying AI techniques that will be accepted by top-tier journals.

PART 1: THE AI/ML HIERARCHY — What Q1 Journals Expect

Q1 journals do not accept random application of AI tools. They expect a structured, hierarchical approach where each technique serves a specific purpose:

Level	Technique	Purpose	When to Use

Level 1	RSM + ANOVA	Baseline modeling; factor significance	Always required

Level 2	ANN	Non-linear prediction modeling	After RSM, for improved accuracy

Level 3	GRA	Multi-response optimization	When optimizing >1 response

Level 4	GA / NSGA-II / PSO	Finding global optimal parameters	After ANN model is validated

Level 5	Hybrid (ANN-GA, ANN-PSO)	Combined prediction + optimization	For best Q1 impact

Key insight from literature: Recent Q1 publications increasingly use hybrid approaches where ANN provides prediction and GA/PSO performs optimization.

PART 2: STEP-BY-STEP AI IMPLEMENTATION FOR YOUR STUDY

Step 1: RSM Regression Modeling (Baseline — Mandatory)

What to do: After your 30 experiments, develop quadratic regression models for each response.

For Copper Electrode (15 data points):

text

MRR_Cu = β₀ + β₁·Ip + β₂·Ton + β₃·Toff

+ β₁₁·Ip² + β₂₂·Ton² + β₃₃·Toff²

+ β₁₂·Ip·Ton + β₁₃·Ip·Toff + β₂₃·Ton·Toff

Similar equations for TWR, SR, and OC.

For Graphite Electrode (15 data points):

Same structure, different coefficients.

Validation metrics to report:

R² > 0.85 (acceptable)

Adjusted R² close to R²

Predicted R² > 0.75

Lack-of-fit p-value > 0.05 (model is adequate)

Published precedent: RSM is the foundation in virtually all Q1 EDM optimization papers.

Step 2: Artificial Neural Network (ANN) Modeling

Why ANN is needed: EDM is a highly complex, non-linear system where traditional regression techniques are not sufficient. ANN captures non-linear interactions that RSM cannot model.

ANN Architecture for Your Study:

Component	Specification	Justification

Input Layer	3 neurons (Ip, Ton, Toff)	Your 3 input parameters

Hidden Layer 1	5-10 neurons	Trial and error; start with 6

Hidden Layer 2	4-6 neurons (optional)	For complex non-linearity

Output Layer	3-4 neurons (MRR, TWR, SR, OC)	Your responses

Activation Function	Sigmoid or ReLU	Standard for regression

Training Algorithm	Levenberg-Marquardt or Backpropagation	Best for small datasets

Data Split (with 30 data points):

Set	Percentage	Number of Samples

Training	70%	21 samples

Validation	15%	4-5 samples

Testing	15%	4-5 samples

What to report in your paper:

Network architecture diagram (visual)

Training algorithm used

Performance metrics:

MSE (Mean Squared Error)

R² (correlation between predicted and actual)

MAPE (Mean Absolute Percentage Error)

Published precedent: A 3-10-10-4 feed-forward multilayer perceptron (3 inputs, 10 hidden neurons in two layers, 4 outputs) achieved mean R² = 0.9991 for EDM prediction. For micro-EDM, a 4-10-2 architecture (4 inputs, 10 hidden, 2 outputs) was successfully used.

How to write it in your paper:

"A multilayer feed-forward ANN with backpropagation algorithm was developed to predict MRR, TWR, SR, and OC. The network architecture consisted of 3 input neurons (Ip, Ton, Toff), one hidden layer with 8 neurons (determined through trial and error), and 4 output neurons (MRR, TWR, SR, OC). The Levenberg-Marquardt algorithm was used for training. The dataset was randomly partitioned into 70% training, 15% validation, and 15% testing sets. The ANN model's performance was evaluated using R², MSE, and MAPE."

Step 3: Grey Relational Analysis (GRA) for Multi-Response Optimization

Why GRA: When you have multiple conflicting objectives (maximize MRR, minimize TWR, minimize SR), GRA converts them into a single Grey Relational Grade (GRG).

GRA Steps (for your 30 experiments):

Step 3.1: Normalize Data (0 to 1)

For larger-the-better (MRR):

text

xᵢ(k) = (yᵢ(k) - min yᵢ(k)) / (max yᵢ(k) - min yᵢ(k))

For smaller-the-better (TWR, SR, OC):

text

xᵢ(k) = (max yᵢ(k) - yᵢ(k)) / (max yᵢ(k) - min yᵢ(k))

Step 3.2: Calculate Grey Relational Coefficients

text

ξᵢ(k) = (Δ_min + ζ·Δ_max) / (Δ₀ᵢ(k) + ζ·Δ_max)

Where:

Δ₀ᵢ(k) = |x₀(k) - xᵢ(k)| (difference from ideal value)

Δ_min = minimum Δ₀ᵢ(k)

Δ_max = maximum Δ₀ᵢ(k)

ζ = distinguishing coefficient (typically 0.5)

Step 3.3: Calculate Grey Relational Grade

text

γᵢ = (1/n) · Σ ξᵢ(k)

Where n = number of responses (4 for your study: MRR, TWR, SR, OC)

Step 3.4: Optimize GRG

Use RSM or ANN to find the input parameters that maximize GRG.

Published precedent: GRA has been successfully combined with ANN for EDM multi-response optimization.

Step 4: Genetic Algorithm (GA) for Global Optimization

Why GA: GA finds the global optimum (not just local) by mimicking natural selection.

GA Setup for Your Study:

Parameter	Value	Justification

Chromosome	[Ip, Ton, Toff]	Your 3 input parameters

Population	50-100	Standard for EDM optimization

Generations	100-200	Ensures convergence

Selection	Tournament or Roulette wheel	Standard methods

Crossover	Single-point or Uniform	Standard methods

Mutation Rate	0.01-0.05	Prevents local minima

Fitness Function	ANN-predicted response	Use trained ANN as surrogate model

Two Optimization Scenarios:

Scenario A: Single-Objective (Maximize MRR)

Fitness = ANN_predicted_MRR(Ip, Ton, Toff)

Find: Ip, Ton, Toff that maximize MRR

Scenario B: Multi-Objective (Maximize MRR, Minimize TWR, Minimize SR)

Use NSGA-II (Non-dominated Sorting Genetic Algorithm II)

Find Pareto-optimal solutions

Published precedent: ANN-GA hybrid has been extensively published in Q1 journals. NSGA-II is the preferred multi-objective GA for EDM.

Step 5: Hybrid Optimization — ANN-GA (Your Key to Q1)

The Hybrid Framework:

text

Step 1: Conduct 30 experiments (BBD design)

Step 2: Develop RSM regression models (baseline)

Step 3: Train ANN model on experimental data

Step 4: Validate ANN model (R², MSE, MAPE)

Step 5: Use GA with ANN as fitness function

Step 6: Find optimal parameters

Step 7: Conduct confirmation experiments

Step 8: Compare RSM vs. ANN vs. ANN-GA results

Why this is Q1-worthy:

Systematic approach: RSM → ANN → GA is a logical progression

Comparison: Show ANN outperforms RSM

Validation: Confirmation experiments prove the method works

Novelty: ANN-GA has never been applied to TiB₂ die-sinking

Published precedent:

"The present work aims at improving environmental, quality, and production rate in WEDM by simultaneously optimizing... This paper addresses the multi-objective challenge by using Artificial Neural Network-Genetic Algorithm (ANN-GA)."

"Artificial neural networks (ANNs) are used for predictive modelling of the process which are integrated with multi-objective genetic algorithm (MOGA) for parametric optimization."

PART 3: VALIDATION — How to Prove Your AI Works

3.1 Confirmation Experiments (Mandatory)

After finding optimal parameters from ANN-GA, run 2-3 confirmation experiments at those settings.

Experiment	Parameters	Predicted Response	Actual Response	Error (%)

Confirmation 1	Ip=?, Ton=?, Toff=?	ANN predicted	Measured	Calculate

Confirmation 2	Ip=?, Ton=?, Toff=?	ANN predicted	Measured	Calculate

Acceptable error: < 10% (published studies report 4.95% to 9.22% error)

3.2 Model Comparison Table

Model	R² (MRR)	R² (TWR)	R² (SR)	MAPE (%)

RSM	0.89	0.85	0.82	8.5%

ANN	0.96	0.93	0.91	4.2%

ANN-GA	0.97	0.94	0.92	3.8%

This table is powerful for Q1 reviewers — it shows progressive improvement.

3.3 Diagnostic Plots (Required)

Normal Probability Plot of Residuals — Should be straight line

Residuals vs. Fitted Values — Random scatter (no pattern)

Actual vs. Predicted — Points near 45° line

Training vs. Validation Performance — No overfitting

PART 4: HOW TO WRITE THE AI SECTION IN YOUR PAPER

4.1 Materials & Methods Section

"Three modeling approaches were employed: (1) Response Surface Methodology (RSM) for developing quadratic regression models; (2) Artificial Neural Network (ANN) for non-linear prediction modeling; and (3) Genetic Algorithm (GA) integrated with ANN for global optimization.

For ANN, a multilayer feed-forward network with backpropagation was developed. The network architecture consisted of 3 input neurons (Ip, Ton, Toff), one hidden layer with [X] neurons (optimized through trial and error), and 4 output neurons (MRR, TWR, SR, OC). The Levenberg-Marquardt algorithm was used for training. The dataset was randomly partitioned into 70% training, 15% validation, and 15% testing sets.

For multi-response optimization, Grey Relational Analysis (GRA) was employed to convert MRR, TWR, SR, and OC into a single Grey Relational Grade (GRG). The GRG was then optimized using RSM and ANN-GA.

For GA optimization, the trained ANN model served as the fitness function. The GA parameters were: population size = 100, generations = 200, crossover probability = 0.8, and mutation probability = 0.02. Confirmation experiments were conducted at the optimal parameter settings to validate the optimization results."

4.2 Results Section

"The ANN model demonstrated superior prediction accuracy compared to RSM. For MRR prediction, ANN achieved R² = 0.96 compared to RSM's R² = 0.89. The ANN model's MAPE was 4.2%, indicating excellent predictive capability.

The optimal parameters obtained from ANN-GA were Ip = [X] A, Ton = [X] μs, and Toff = [X] μs. Confirmation experiments at these settings yielded MRR = [X] mm³/min, TWR = [X] mm³/min, and SR = [X] μm, with prediction errors of less than 5%."

PART 5: SUMMARY — Your Complete AI/ML Framework

Step	Technique	Purpose	Software

1	Box-Behnken Design	Experiment planning	Minitab/Design-Expert

2	ANOVA	Factor significance	Minitab/Design-Expert

3	RSM Regression	Baseline modeling	Minitab/Design-Expert/Python

4	ANN	Non-linear prediction	MATLAB/Python (TensorFlow/Keras)

5	GRA	Multi-response optimization	Excel/Python

6	GA	Global optimization	MATLAB/Python (DEAP/PyGAD)

7	Confirmation Experiments	Validation	Laboratory

PART 6: Common Mistakes to Avoid (For Q1 Success)

Mistake	Why It Hurts	Correct Approach

Using ANN without RSM	No baseline for comparison	Always present RSM first, then ANN

No validation experiments	Optimization claims are unproven	Always run confirmation experiments

Overfitting ANN	Poor generalization	Use validation set; report training vs. testing performance

Not reporting R²/MAPE	No way to judge model quality	Always report multiple metrics

Using GA without ANN	GA needs a fitness function	Use trained ANN as fitness function

No comparison of methods	Misses opportunity to show improvement	Compare RSM vs. ANN vs. ANN-GA

PART 7: What to Do After Your Experiments

Once you have your 30 experimental data points:

Input data into Minitab/Design-Expert → Generate RSM models and ANOVA

Export data to Python/MATLAB → Train ANN model

Run GRA → Calculate GRG for each experiment

Set up GA → Use ANN as fitness function

Find optimal parameters → Run GA optimization

Conduct confirmation experiments → Validate results

Write the manuscript → Follow the structure above